FEATURES

- Produce more than 14 watts of power (Th=250°C, Tc=50°C)

- Intermittent Operation beyond 350°C

- Intermittent Power up to 25 watts

- Rugged Construction (no ceramic, no solders, fiber reinforced construction makes module tolerant to abuse)

- Long life (> 10 years when properly used)

- 126 couples (Bi,Sb)2(Te,Se)3)

- Produce 10mW @ ΔT=5°C

- Notches for easy alignment

DESCRIPTION

This module is designed specifically for the generation of power and is able to tolerant intermittent temperatures exceeding 350°C but for maximum life expectancy it should not exceed 250°C. These high temperature properties are made possible by the bonded metal conductors that eliminate the presence of all solders.

While the module is optimized for waste heat recovery its reversible properties make it suitable as a thermoelectric cooler, especially for high temperature applications where sensitive electronic equipment must be cooled to below the ambient temperatures.

| Thermal and Electrical Characteristics |
| --- |
| Parameter | Conditions | min typ max | units |
| Power | Th=250°C, Tc=50°C @matched load | 14.0 15.5 17.0 | Watts |
| Open Circuit Voltage | Th=250°C, Tc=50°C | 7.6 8.0 8.4 | Volts |
| Matched load Voltage | Th=250°C, Tc=50°C | 3.8 4.0 4.2 | Volts |
| Internal Resistance | Th=250°C, Tc=50°C | 0.9 1.0 1.1 | Ω |
|  | T = 25°C | 0.55 0.6 0.65 | Ω |
| Current | Th=250°C, Tc=50°C @matched load | 3.8 4.0 4.2 | Amps |
|  | Th=250°C, Tc=50°C @short circuit | 7.6 8.0 8.4 | Amps |
| Heat Flux | Th=250°C, Tc=50°C @matched load | 410 430 450 | Watts |
|  | Th=250°C, Tc=50°C open circuit | 200 210 220 | Watts |
| Heat Flux Density | Th=250°C, Tc=50°C @matched load | 12 13 14 | W/cm2 |

# Text boxes

Stated temperatures are assumed to be on the module surface and not the heat exchangers.

Module surfaces are conductive and require the use of an insulator when used against metal heat exchangers. Ceramic wafers with thermal grease provide optimum performance.

Recommended mounting pressure is 100 to 200 psi uniformly distributed over the module surface.