FEATURES

- Produce more than 20 watts of power (Th=250°C, Tc=50°C)

- Intermittent Operation beyond 350°C

- Intermittent Power up to 30 watts

- Rugged Construction (no ceramic, no solders, fiber reinforced construction makes module tolerant to abuse)

- Long life (> than 10 years when properly used)

- 71 couples (Bi,Sb)2(Te,Se)3)

- Produce 15mW @ ΔT=5°C

DESCRIPTION

This module is designed specifically for the generation of power and is able to tolerant intermittent temperatures exceeding 350°C but for maximum life expectancy it should not exceed 250°C. These high temperature properties are made possible by the bonded metal conductors that eliminate the presence of all solders.

While the module is optimized for waste heat recovery its reversible properties make it suitable as a thermoelectric cooler, especially for high temperature applications where sensitive electronic equipment must be cooled to below the ambient temperatures.

| Thermal and Electrical Characteristics |
| --- |
| Parameter | Conditions | min typ max | units |
| Power | Th=250°C, Tc=50°C @matched load | 20.0 21.0 22.0 | Watts |
| Open Circuit Voltage | Th=250°C, Tc=50°C | 4.2 4.5 4.8 | Volts |
| Matched load Voltage | Th=250°C, Tc=50°C | 2.1 2.25 2.4 | Volts |
| Internal Resistance | Th=250°C, Tc=50°C | 0.24 0.25 0.26 | Ω |
|  | T = 25°C | 0.14 0.15 0.16 | Ω |
| Current | Th=250°C, Tc=50°C @matched load | 9.0 9.5 10.0 | Amps |
|  | Th=250°C, Tc=50°C @short circuit | 18.0 19.0 20.0 | Amps |
| Heat Flux | Th=250°C, Tc=50°C @matched load | 450 475 500 | Watts |
|  | Th=250°C, Tc=50°C open circuit | 310 325 340 | Watts |
| Heat Flux Density | Th=250°C, Tc=50°C @matched load | 9 10 11 | W/cm2 |

# Comments

tolerate

need comma ‘,'

Y axis label for efficiency graph, match load efficiency or maximum efficiency? Percentage symbol. Some tests need to be done to update this graph.

# Text boxes

Stated temperatures are assumed to be on the module surface and not the heat exchangers.

Module surfaces are conductive and require the use of an insulator when used against metal heat exchangers. Ceramic wafers with thermal grease provide optimum performance.

Recommended mounting pressure is 100 to 200 psi uniformly distributed over the module surface.